## Slide 1
بسم الله الرحمان الرحيم

## Slide 2: PRODUCTION OF FERROUS METALS Cast iron
1 - Development of the steel industry
2- Cast iron production
3 - Raw materials
4 - Blast furnace
5 - Standard designation of cast irons

## Slide 3
1 - Development of the steel industry
To transform iron ore into metal, the first metallurgists used rudimentary earthen furnaces: the "low furnaces".
These furnaces were simply made up of a hole lined with stones where iron ore and charcoal were piled up in alternating layers, the whole covered with a layer of clay.
The iron oxide, collected from the ground, was in the form of small rocks.
This furnace was lit and a not very effective blowing was carried out using hollow rods.

## Slide 5
2- Cast iron production
Industrial process with blast furnaces (80 m high,
5000 cubic meters, temperatures of 1600 degrees, and continuous production up to 10000 tons per day…).
A blast furnace never stops during the 10 years of its existence.
Blast furnace of ANNABA

## Slide 6
4 - Raw materials
The raw materials intended for the production of primary cast iron are:
Iron ore. Coke. Fluxes.

## Slide 7
coke and additions sector
It receives the coke (at the port of Annaba) by truck, stores, processes and transports the fuels and additions necessary for the operation of the blast furnaces.

## Slide 8
Homogenization:
The heap consists of mixing several constituents including the ore with the additions using a thrower (storage machine)

## Slide 9
Blast furnace of ANNABA

## Slide 10
Blast furnace of ANNABA

## Slide 11
Blast furnace of ANNABA

## Slide 12
Blast furnace
(cast iron production)
iron ore
fluxes (lime)
coal coke
PRINCIPLE

## Slide 13
5 - Blast furnace
It consists of the following parts
from bottom to top:
1- The crucible
2- The tank
3- The belly
4- The display
5- The throat
6- Metal shielding

## Slide 14
5 - Blast furnace
1- The crucible: cylindrical part, the upper part of which is called the work and carries the pipes that bring the hot air.
2- The tank: truncated cone flared towards the bottom.
3- The belly: cylindrical part.
4-The display: truncated cone flared towards the top
5- The throat: opening through which the charge is introduced and from which the gases escape.
6- Metal shielding with the same profile as the blast furnace

## Slide 15
Transformation inside the blast furnace
Dehydration
Dissociation
Decarbonation

## Slide 16: Iron+carbon diagram (Cast iron and Steel)

## Slide 17
The cast irons obtained in the blast furnace are distinguished from each other by their chemical compositions.
Type de fontes H-F | C % | Si % | Mn % | P % | S %
Fonte pauvre en Mn | ≈4% | Jusqu’à 1 | (<1) | 0.08-0,12 | Jusqu’à 0.05
Fonte riche en Mn | ≈4% | Jusqu’à 1 | (2 - 3) | 0.08-0,12 | Jusqu’à 0.05
Fonte Thomas | 3.2 - 3,6 | 0,3 - 0,6 | 0.5 - 1,5 | 1,7-2.2 | 0,05-0.15
Fonte Bessmer | 3.8 | 1.0-2.5 | 1 -3 | 0,07 - 0,1 | Jusqu’à 0.04
Fonte de Fonderie | 3,5 - 4.2 | 2-3 | Jusqu’à 1.0 | 0.5- 1.0 | Jusqu’à 0.07
Fonte Hématite | 3,5 - 4.2 | 2 - 2.5 | 0,7- 1.5 | 0,08-0.12 | Jusqu’à 0.04
Fonte-manganèse | 6-8 | < 1.5 | 3 - 8 | 0.2 - 0.3 | 0.02

## Slide 18
Iron and
steel industry

## Slide 19
The most used metal is iron and its alloys (cast iron and steel), because its technical importance is justified by production statistics

## Slide 20
6 - Standardized designation of Cast irons
Cast irons are divided into two groups according to their method of production, depending on the state of existence of carbon in the form of cementite or graphite.
1 - White cast iron: All the carbon is in the form of cementite Fe3C, obtained when cooling is fast enough and the casting temperature is low enough.
2 - Grey cast iron: All the carbon is free and is in the form of graphite. They are obtained during slow cooling with a high enough casting temperature.

## Slide 22
7- Examples of designation:
1- Ft 10, Ft 15, Ft 20, Ft 25.
2- FGS 370-17, FGS 500-17, FGS 700-2.
3- MB 35 - 10, MB 40 – 12, MN 38 – 18, MN 40 – 20
MP 55 - 5, MP 65 – 8.
4- L – Ni Si Cr 30 – 5 – 5, L – Mn Ti Co 25 – 8 – 7 .

## Slide 23
    Ft 10
  Ft: Grey cast iron with lamellar graphite.
  10: Minimum tensile strength (Rm): 10 daN/mm²
  FGS 370-17
FGS: Spheroidal graphite grey cast iron
370: Minimum tensile strength = 370 N/mm²
17: Elongation (A= 17%)MB 30 – 10
  MN 38 – 18
MN: malleable cast iron, black core
30: Minimum tensile strength Rm = 30 daN/mm²
10: Elongation after rupture A = 10%

## Slide 24
    MB 30 – 10
MB: malleable cast iron, white core
30: Minimum tensile strength Rm = 30 daN/mm²
10: Elongation after rupture A = 10%
    MP 55 – 5
MP: malleable cast iron, with pearlitic core
55: Minimum tensile strength Rm = 55 daN/mm²
5: Elongation after rupture A = 5%
    L – Ni Si Cr 30 – 5 – 5
L: alloyed lamellar cast iron
Ni: Addition element Nickel with 30%
Si: Addition element Silicon with 5%
Cr: Addition element Chromium with 5%

## Slide 25: THANK YOU FOR YOUR ATTENTION